## Slide 1: Review on SC for seminars

## Slide 2: Compensate semiconductors

## Slide 4: Degenerate semiconductors
1. The doping concentration is so high that EF moves within a few kT of the band edge (EC or EV). Boltzman approximation not valid.
2. High donor concentrations cause the allowed donor wavefunctions to overlap, creating a band at Edn.
First only the high states overlap, but eventually even the lowest state overlaps.
This effectively decreases the bandgap by DEg = Eg0 – Eg(ND).
Refers to SC: whouse electron mobility decreases as temperature increases;
That has a band gap smaller than its equilibrium Fermi level
Degenerate SC conduct electricity even at lower temperatures

## Slide 5: As the doping conc. increases more, EF rises above EC
EV
EC (intrinsic)
available impurity band states
EF
DEg
EC (degenerate) ~ ED
filled impurity band states
apparent band gap narrowing:
DEg* (is optically measured)
-
Eg* is the apparent band gap:
an electron must gain energy Eg* = EF-EV
Degenerate Semiconductors

## Slide 6: Electron Concentration in degenerately doped n-type semiconductors

## Slide 7: Equilibrium electron and hole concentrations

## Slide 8: Position of Fermi energy level

## Slide 11: A very useful relationship
…which is independent of the Fermi Energy
Recall that ni = no= po for an intrinsic semiconductor, so
nopo = ni2
for all non-degenerate semiconductors.
(that is as long as EF is not within a few kT of the band edge)

## Slide 12: Summary
non-degenerate:
The intrinsic carrier density: nopo= ni2
degenerate n-type:
nopo= ni2 (ND/NC) exp[DEg*)/kT]
degenerate p-type:
nopo= ni2 (NA/NV) exp[DEg*)/kT]
is sensitive to the energy bandgap, temperature, and m*

## Slide 13: Legea Wiedemann–Franz
În fizică, legea spune că raportul dintre contribuția electronică a conductivității termice (κ) la conductivitatea electrică (σ) a unui metal este proporțional cu temperatura (T). [1]
Teoretic, constanta de proporționalitate L, cunoscută sub numele constanta Lorenz, este egală cu :
Această lege empirică a fost numită după Gustav Wiedemann și Rudolph Franz, care în 1853 au raportat că κ/σ are aproximativ aceeași valoare pentru diferite metale la aceeași temperatură. [2] Proporționalitatea lui κ/σ cu temperatura a fost descoperită de Ludvig Lorenz în 1872.

## Slide 14: Rezistenta de patrat /unei foi

## Slide 15: Elemente de cristalografie