## Slide 1: Lectia practica 10 DMOE
Alte probleme

## Slide 2: Solar Cell
2. Consider a Si p-n junction solar sell of area 2 cm2 . If the dopings of the solar cell are Na = 1.7 × 10^16 cm−3 and Nd = 5 × 10^19 cm−3 , and given τn = 10 µs, τp = 0.5 µs, Dn = 9.3 cm2/s, Dp = 2.5 cm2/s, and IL = 95 mA,
(i) calculate the open-circuit voltage, and
(ii) determine the maximum output power of the solar cell at room temperature

## Slide 4
3. At room temperature, an ideal solar cell has a short-circuit current of 3 A and an open-circuit voltage of 0.6 V.
Calculate and sketch its power output as a function of operation voltage and find its fill factor from this power output.

## Slide 6
4. What happens to the short-circuit current, the open-circuit voltage, and the maximum output power of the solar cell from the previous problem if it is employed as a power supply for the Mars Pathfinder mission?
Mean distance from the Mars to the Sun is approximately a factor of 1.5 longer than that of between the Earth and the Sun.
Assume that in both cases the solar cell operates at room temperature.

## Slide 7
4. Since the flux density depends as r^−2 from the distance to the Sun, the short-circuit current is IL(Mars) = IL(Earth) /1.5^2 = 1.33 A. The open-circuit voltage is then
From here, we find Vm = 0.5 V and, thus, Pm = VmIm = 0.61 W

## Slide 8
5. At room temperature, an ideal solar cell has a short-circuit current of 2 A and an open-circuit voltage of 0.5 V.
How does the open-circuit voltage change if the shortcircuit current drops by a factor of 2, 5, or 10?

## Slide 9
5. From the parameters given, we find that
Is ≈ IL exp(−eVoc/kT) = 4.1 × 10^−9 A.
Therefore, Voc = 0.48, 0.46, and 0.44 V, for IL = 1, 0.4, and 0.2 A, respectively.

## Slide 10
6. At 300 K, an ideal Si p-n junction solar cell has a short-circuit current of 2 A and an open-circuit voltage of 0.5 V.
How does the maximum output power of the solar cell change if the temperature raises to 400 K?

## Slide 11
6. From the values of Voc and IL, we find that at 300 K Is ≈ IL exp(−eVoc/kT) = 4.1 × 10−9 A.
Employing the results of the previous problems, we find that the maximum output power at 300 K is equal to 0.8 W. In the case of a p-n junction Is ∼ ni^2 ∼ exp(−Eg/kT). Since for Si Eg = 1.12 eV, we obtain that Is = 0.2 mA when the temperature raises to 400 K. The new value of Is corresponds to Voc = 0.3 V.
Finally, we get that the maximum output power of the Si solar cell at 400 K drops down to 0.4 W.