## Slide 1: Tema 26 Instrumentatie si metrologie pentru nanotehnologii
Precision DC Current, Voltage and Resistance Measurements

## Slide 2: Instrumentatie si Metrologie pentru Nanocaracterizare

## Slide 3: SCOP
Nanocaracterizarea acoperă probleme din metrologia fizică și chimică, inclusiv măsurători ale forței și lungimii, determinarea compoziției chimice, formelor porilor și particulelor și 3D relații ale componentelor complexe la scară nanometrică.
Pentru a sprijini promovarea nanotehnologiei în industrie, sunt necesare progrese în nanocaracterizare, inclusiv:
•Dezvoltarea expertizei de măsurare adecvate
•Realizarea capacităților de imagistică 3D la scară nanometrică
•Achiziția de metode de măsurare care sunt acceptate științific și fără artefacte
•Disponibilitatea metrologiei cantitative cu capacități analitice care sunt complementare privind prezentarea la microscara
Va fi necesară o combinație de capabilități de măsurare pentru a aborda provocările nanocaracterizării.
Acestea fie vor extinde tehnicile de măsurare existente, cum ar fi cele utilizate de microscopiști și spectroscopiști, sau vor apărea noi metode de măsurare care permit factorilor de compoziție și de performanță să fie cantitativi și reproductibili la măsurători la scară nanometrică.

## Slide 4: CURRENT SCIENTIFIC AND TECHNOLOGICAL ADVANCEMENTS
•Demonstrarea sensibilității chimice și cartografierii la scară atomică.
•Tomografie pentru determinarea morfologiei și structuriifoarte mici organice și biostructurilor precum și pentru materiale și dispozitive neorganice.
•Holografie electronică pentru imaginea și măsurarea proprietăților electrice, magnetice și de grosime la rezoluție înaltă.
•Instrumente de caracterizare și fabricare cu dublă utilizare, cum ar fi fascicul de ioni focalizat cu fascicul dublu (FIB) și scanarea cu sonde ne permit să tăiem, să frezăm, să mutăm, să lipim și să plasăm bucăți, linii și chiar la scară nanometrică atomi pentru construirea și modelarea nanodispozitivelor și artefactelor simple în același timp cu imaginea și caracterizarea lor.
•Debitul de mostre, inclusiv colectarea și interpretarea datelor, a crescut dramatic. La fel un exemplu, TEM a trecut de la aproximativ studierea unui speciment la câteva zile la, uneori la peste 10 exemplare pe zi în fabricile de semiconductori.
As a sample preparation tool, the Dual Beam FIB-SEM has revolutionized sample preparation for SEM and TEM samples by making more precise cross sections, expanded the use of FIB by allowing for simultaneous preparation, imaging, and elemental analysis, and has allowed for more accurate cross sectioning for previously hard-to-section materials and products. Dual Beam FIB can essentially be used for any type of materials analysis, including but not limited to semiconductors, batteries, medical devices, aerospace, and more.

## Slide 5
Trade-off of trace species detection with
spatial resolution
Trade-off of depth resolution versus lateral resolution

## Slide 6
Trade-off of chemical specificity with spatial resolution
Near-field Raman image of a single-walled carbon nanotube (SWNT) and associated Raman scattering spectrum.

## Slide 7: Key Challenges and Barriers for Nanocharacterization
Metrology | Challenges/Barriers
Chemical Compozition | Multiphase capability • Merging of data from multiple measurements • Standards and calibration • Resolution, sensitivity, and speed
3D characterization of Structures | Spatial and spectral resolution and specificity • Data acquisition speed and throughput limitations • Synthesis of 3D information from 2D datasets • Merging of data from different metrology tools • Measurement artifacts
Dispersion of Materials in a Matrix | • Non-existent techniques for examining dispersibility of nanomaterials in a matrix • Poor sensitivity, slow, non-scalable methods
Interface Characterization | Non-destructive characterization • Buried or embedded interfaces • Interface stability • Probe robustness • Preserving process/sample in situ
Speed of Characterization | • Detector speed, efficiency and sensitivity • Source brightness • Software for smart analysis, fast data collection and processing • Fast automated sample preparation
Sample Preparation and Handling | • Inability to extract information about 3D arrangement of atoms • Manipulation of particles • Non-destructive sample sectioning

## Slide 8: Nanocharacterization Grand Challenge Three-Dimensional Characterization of Individual Nanostructures

## Slide 9: Vision and Goals (Cont.)

## Slide 10: Nanocharacterization Grand Challenge Speed of Characterization

## Slide 11: Cont

## Slide 12: Nanocharacterization Grand Challenge Interface Characterization

## Slide 14: Nanocharacterization Grand Challenge In situ Characterization of Interface Phenomena

## Slide 16: Nanocharacterization Grand Challenge Quantitative Measurement of Dispersion of Nanoscale Materials in a Matrix

## Slide 18: Nanocharacterization Grand Challenge Measuring Processes Inside Cells and Tracking Particles in Living Tissue

## Slide 20: INSTRUMENTATION AND METROLOGY FOR NANOMECHANICS
DOMENIUL DE APLICARE
Provocările științifice și tehnice din nanomecanică acoperă un spectru de domenii de cercetare interdisciplinare transfersale și de aceea necesită o gamă largă de instrumente și metrologie. Provocările științifice în nanomecanica pot include, de exemplu, proiectarea de noimateriale cu proprietăți mecanice noi bazate pe nanostructuri adaptate sau înțelegerea proprietățile mecanice și modului răspunsurilor precum rigiditatea, duritatea și duritatea la rupere care evoluează neliniar în cadrul unor rețele de nanosisteme sau componente.
Instrumentatia pentru nanomecanica poate trebuie să caracterizeze atomii de la interfețe și suprafețe din materialele la scară nanometrică aplicate solicitări sau pentru a explora comportamentul mecanic al sistemelor funcționale la scară nanometrică, cum ar fi cele biologice și obiecte biomoleculare.
Metrologia avansată poate fi utilizată pentru interpretarea mecanică a comportamentului neobișnuit (tărie care se apropie de limitele teoretice, coeficienți de aderență inversați cu sarcina) la scale de lungime nanometrică.
Prin urmare, acest subiect acoperă probleme tehnice specifice asociate cu cele mai frecvente trei metode utilizate în prezent pentru obținerea datelor de proprietăți mecanice la scară nanometrică - microscopie cu sondă de scanare (SPM), nanodentație și nanotribologie, dar abordează și problema de viitoare instrumentare. Tehnici precum difracția, împrăștierea cu unghi mic, transmisia, reflectometrie, împreună cu instrumente de mediu, rheometrele și echipamentele de stres aplicate (tensiune, compresie și torsiune) etc

## Slide 21: Realizarea viziunii pentru nanomecanica va necesita
•Standarde globale care includ calibrarea primară, utilizarea artefactelor de calibrare, metode de teste standarde metode standardizate de analiză a datelor
•Eșantioane de testare, platforme și tehnici de testare care permit măsurarea mecanică a proprietăți în medii reale de aplicare și la scări de lungime adecvate
•Modele care permit o conexiune cantitativă între măsurătorile mecanice la scară nanometrică și proprietățile materiale relevante
•Instrumentare multi sondă care oferă informații mecanice detaliate în timpul și după măsurători de proprietăți nanomecanice pentru interpretarea corectă a datelor; de exemplu, modificările microstructurale și modificările chimice ca urmare a sondei mecanice trebuie să fie monitorizate și înțelese pentru a evita interpretarea greșită a rezultatelor
•Platforme de metrologie automate care permit o rezoluție integrată, multifuncțională și spațială rapidă, măsurători și analize nanomecanice rapide
Direct measurements of atomic bonding forces often involve consideration of different possible crystalline structures at contacts, as illustrated by these three configurations of a Au nanowire

## Slide 22: Current State of the Art of Nanomechanical Instrumentation
Instrumentation | Accuracy | Sensitivity | Resolution | Precission | Compatibility with Different Material System
Scanning Probe Microscopes | • Greatest challenge • Calibration-dependent • Tip and surface damage contributes to poor accuracy | • Piconewton to nanonewton range • Can be enhanced Through chemical Modification of the tip | • Subnanometer • Dependent on scanning mode and sharpness of tip | • Dependent on cantilever, environment, and scanner performance | • Limited to materials with E > 109 Pa
Instrumented Indentation Testing | • Large uncertainties at small forces and displacements • Model-dependent results | • Nanonewton to Millinewton range • Can be enhanced by Harmonic Oscillation | • Large tips not conducive to nanoscale measurement | • Highly dependent on tip shape Knowledge | • Limited to materials with E > 106 Pa
Tribometers and Nanoscratch Testers | • Real area of contact determination is the major limitation • Higher requirements in rigidity because lateral resistance can be large • Force sensors are more sensitive than instrumented indentation testing but less than scanning probe microscope | • Nanonewton to Millinewton range • Vibration and Environmental factors affect results significantly • Large variety of tips and cantilever Designs | • Depends on tip sizes • Most tips are suitable for microscale measurements • Advanced diamond tips can get below 50 nm radius | • Depth of penetration during sliding can be controlled only to several nanometers • Dependent on Environmental control and vibration Isolation | • Limited by surface roughness at nanometer Scale • Materials limited by tip hardness and system Stiffness

## Slide 23: Key Challenges and Barriers for Nanomechanics
Metrology | Chalenges / Barriers
Standards and Calibration | • Traceable force and displacement calibration • International collaboration to establish common standards • Methodologies based on reliable data and models • Machine-independent standards • Understanding of nanometer scale surface forces and contact mechanics • Wide experimental dynamic range
Nano-mechanical Modeling of Experiments | • Modeling—computational power, intelligent data storage and mining, length of model development time, capturing physics • Experiment—ability to fabricate and characterize testing fixtures, manufacture and characterize samples; accuracy and traceability for experiments; ability to position/manipulate samples
Integration of Multiple Technique | • In situ probes for imaging, manipulation, chemical bonding and orientation detection at atomic/molecular resolution • Spatial resolution when focusing on a single event • Integration of software, input/output compatibility, control languages • Synchronization of time and position information
High- Throughput Automated Measurements | • Sample preparation—speed, automation, yield, quality, size, conditioning, and material specific issues (polymers, metals, ceramics, glasses, electronics) • Calibration—robust probes, periodic reference specimens or characterizations • Analysis/testing schemes—lack of wide range of testing environments (temperature, frequency); lack of models to describe complex nanoscale mechanical behavior; lack of high-speed methodologies; lack of well-characterized nanoscale probes
Instrument Development | • Tip wear, control, cm to nm positioning • Decoupled lateral and vertical force sensors • Lack of lateral or vertical force calibration standards • Multiple operating mechanisms and environments required for mechanical property measurements • Non-linearity of actuators/sensors • Thermal drift • Quantitative mechanical property mapping is typically a slow, point-by-point process
Measurement Under Real Application Conditions | • Real area of contact • Surface treatments • Robustness • Application-compatible materials • Real-time measurement capabilities • Sub-element specific testing (e.g., interfaces)

## Slide 24: Nanomechanics Grand Challenge Standards and Calibration

## Slide 26: Nanomechanics Grand Challenge Nanomechanical Modeling of Experiments

## Slide 28: Nanomechanics Grand Challenge Integration of Multiple Techniques

## Slide 30: Nanomechanics Grand Challenge High-Throughput Automated Nanomechanical Measurements

## Slide 32: Nanomechanics Grand Challenge Instrument Development for Nanomechanics

## Slide 34: Nanomechanics Grand Challenge Mesurement under Real Application Conditions

## Slide 36: Instrumentation and Metrology for Nanoelectronics, Nanophtonics, and Nanomagnetics

## Slide 38: Nanophotonics